**Title: Evaluation Of Chemical Composition Of Root Canal Dentin Between Two Age Groups Using Different Irrigating Solutions: An In Vitro SEM-EDS Study.**

**Cover letter**

**TO,**

**The Editorial Board,**

**Journal of Oral Health and Research Dentistry.**

**I would like to submit the manuscript entitled “Evaluation Of Chemical Composition Of Root Canal Dentin Between Two Age Groups Using Different Irrigating Solutions: An In Vitro SEM-EDS Study.” an Original research article by the author names mentioned below in the the journal of Oral Health and Research Dentistry.**

**We declare that this manuscript is original has not been published before and is considered for publication elsewhere. We know of no conflicts of interest and no financial support and as a corresponding author I confirm that the manuscript has been read and approved for submission by all authors.**

**Thank you.**

**AUTHORS DETAILS AND AFFLIATIONS**

**1.Dr.Kallu Abhijith MDS,Assistant Professor, SVS Institute of Dental Sciences,Mahabubnagar.**

**Speciality: Conservative Dentistry and Endodontics**

**Mail id:drabhijithkallu@gmail.com**

**Orchid no:0009-0003-9911-3936**

**2. Dr.L.R.Surender MDS, Professor, SVS Institute of Dental Sciences,Mahabubnagar.**

**Speciality: Conservative Dentistry and Endodontics**

**Mail id:lsurender@yahoo.com**

**Orchid no:0000-0002-5640-3066**

**3. Dr.Sravani Nirmala MDS, Assistant Professor, SVS Institute of Dental Sciences,Mahabubnagar.**

**Speciality: Conservative Dentistry and Endodontics**

**Mail id:drsravaninirmala87@gmail.com**

**Orchid no:0000-0002-5623-0855**

**4. Dr.Naresh Kumar MDS, Reader, SVS Institute of Dental Sciences,Mahabubnagar.(CORRESPONDING AUTHOR).**

**Speciality: Conservative Dentistry and Endodontics**

**Mail id:20kmrknrsh@gmail.com**

**Orchid no:0000-0001-6734-6071**

**5. Dr.Narender Reddy MDS, Professor, SVS Institute of Dental Sciences,Mahabubnagar.**

**Speciality: Conservative Dentistry and Endodontics**

**Mail id:mail2drreddy@gmail.com**

**Orchid no:0000-0002-4960-2489**

**6.Dr.Chukka Rakesh Reddy MDS,Associate Professor, SVS Institute of Dental Sciences,Mahabubnagar.**

**Speciality: Conservative Dentistry and Endodontics**

**Mail id:chukkarakesh@gmail.com**

**Orchid no:0000-0002-4790-204X**

**INTRODUCTION:**

The key to successful endodontic therapy is to ensure complete eradication of microbial volume, which can be accomplished by cleaning and shaping phase of root canal therapy [1]. Biomechanical preparation leads to accumulation of organic pulpal material and inorganic dentinal debris producing an amorphous, irregular surface layer known as “Smear layer”[2]. The bacterial harbouring potential of smear layer within dentinal tubules prevents proper disinfection as well as penetrability of sealer and adhesion of obturation materials[3].

Irrigation is considered to be a vital adjunct to instrumentation of root canals. Hence, it has been agreed that “*files shape and irrigants clean”* [4].Sodium hypochlorite (NaOCl), commonly used irrigation agent has a potential to dissolve organic matter and necrotic tissue, also prevents greater dentin dissolution, but leaves a smear layer of mineralized tissue [5]. MTAD (Mixture of Tetracycline Isomer, Acid and Detergent) a synergistic combination of 3% doxycycline, 4.25% citric acid and detergent (Tween-80) introduced by Torabinejad had significantly improved smear layer removal as it is considered to be a chelating agent and also induces inconsiderable erosion.A new formulation of EDTA (Ethylene Diamine Tetraacetic Acid), SmearClear containing 17% EDTA, Cetrimide and a specific surfactant have gained increasing attention in recent years [6].

Dentin composition is described based on its organic and inorganic constituents. Calcium and phosphorus present in hydroxyapatite crystals are considered to be the major inorganic components of dental hard tissues. Any change in the Ca/P ion ratio may alter the standard proportion of the organic and inorganic components in the dentin which in turn affects the micro-hardness, permeability as well as solubility characteristics of dentin, sealing ability and adhesion of dental material to the root canal dentin[7].

Age-related changes of the dentin while performing endodontic therapy are considered to be critical for the success of the treatment. The continuous deposition of peritubular dentin, consequent narrowing of dentinal tubules, and a decrease in the number of dentinal tubules are commonly seen among older individuals as these changes tend to correlate with the natural ageing process of humans[8].

Various studies interpolating the above factors have been primarily focused only on efficiency of root canal irrigants on the chemical composition of dentin. Hence, the present study aimed to evaluate and compare the effect of different irrigating solutions on the chemical composition of root canal dentin between two age groups.

**MATERIALS AND METHODS:**

**PREPARATION OF SPECIMENS:**

Sixty-six single rooted human premolar teeth extracted from the subjects aged 18-25 years and 47-65 years, (33 from each group) for orthodontic and periodontal reasons were collected from the Department of Oral and Maxillofacial Surgery, S.V.S. Institute of Dental Sciences, Mahabubnagar. Teeth with open apex, anatomical variations and sharp curvatures were excluded from the study. Surfaces of collected human premolar teeth were visually examined with naked eye for any macroscopic surface defects, cleaned of debris and calculus using an ultrasonic device and stored in distilled water till the experiment was initiated. Specimens from each group were then divided randomly into three subgroups A, B and C (n= 11) based on the irrigant used as follows:

|  |  |  |
| --- | --- | --- |
|  | **GROUP-1**  **Young Group (18-25 years)** | **GROUP-2**  **Old Group (47-65 years)** |
| **SUB GROUP A** | NaOCl | NaOCl |
| **SUB GROUP B** | MTAD | MTAD |
| **SUB GROUP C** | SmearClear | SmearClear |

**EXPERIMENT:**

Decoronation of the teeth was done using a micromotor straight hand piece and diamond disc to standardize root length to 10 mm. Patency of the canal was checked with #10 K-file (fig-9) and canals were instrumented till #15 K-File and subsequently with ProTaper Ni-Ti rotary instrument sequence until master apical file #F3. Between each file, canals were irrigated with 2 mL 3% NaOCl, then irrigated with distilled water and final irrigation is done with:

|  |  |  |
| --- | --- | --- |
|  | **GROUP-1**  **Young Group (18-25 years)** | **GROUP-2**  **Old Group (47-65 years)** |
| **SUB GROUP A** | 1ml of 0.9% Saline for 1 minute | 1ml of 0.9% Saline for 1 minute |
| **SUB GROUP B** | 1ml of MTAD for 1 minute | 1ml of MTAD for 1 minute |
| **SUB GROUP C** | 1 ml of SmearClear for 1 minute | 1 ml of SmearClear for 1 minute |

All samples were then dried with sterile absorbent paper points and grooved longitudinally in a buccolingual plane with a slow speed diamond disc and split into two halves using a chisel and mallet and stored in distilled water until use. The samples from each group are subjected to energy dispersive spectroscopy to determine the alteration in Ca, P, Na and Mg caused by the various irrigants.

**POST EXPERIMENTAL EVALUATION OF MINERAL CONTENT OF SPECIMENS:**

The specimens were secured on metallic (aluminium) stubs, dried in the critical point dryer, sputter coated with gold and analysed under SEM-EDS (JOEL/JSM-IT500A) at 20 kV, in which the specimens are bombarded with a high-voltage electron beam that generates different wavelengths for each type of mineral. The change in wavelength of the radiation that is emitted by the specimens is used to determine the post-experimental atomic percentage of Ca, P, Na, Mg.

**STATISTICAL ANALYSIS:**

Data was entered and analyzed using SPSS (Statistical Package for Social Sciences) software 26.0 (IBM, New York). Descriptive statistics were presented as means and standard deviations for numerical variables, or as frequencies and percentages for categorical variables. Inferential statistics included independent sample t-test for comparison of means between two different age groups. The level of significance was set at p ≤ 0.05.

**RESULTS:**

Results revealed a statistically significant difference in calcium levels of younger age group, with higher levels for SmearClear (19.1±1.31) when compared to MTAD (17.1±1.16), with p value 0.01(Table-1). A statistically significant difference was observed in magnesium levels of younger age group, with higher levels for MTAD (0.95±0.21) when compared to SmearClear (0.82±0.22), with p value 0.05 (Figure-1). Mean comparison of Ca/P ratio of younger age group, revealed higher values for SmearClear (1.71±0.14) when compared to MTAD (1.56±0.15), with p value 0.02 (Table-2).

Independent sample t-test revealed statistically significant difference in phosphorous levels of older age group, with higher levels for SmearClear (13.9±1.90) when compared to MTAD (12.7±1.32), with p value 0.03 (Table-3). Statistically significant difference was observed in magnesium levels and Ca/P ratio of older age group, with higher levels for SmearClear (1.27±0.26) & (1.49±0.30) when compared to MTAD (1.21±0.45) & (1.42±0.24), with p value 0.05 (Figure-2).

**Figure-1 Mean comparison of magnesium content between irrigants within young group**

**Figure-2 Mean comparison of magnesium content between irrigants within old group**

**Table-1 Mean comparison of calcium content between irrigants within young group**

|  |  |  |
| --- | --- | --- |
| **CALCIUM CONTENT** | | |
| **Groups** | **Group 1**  **(Younger age group)** | |
| **Mean** | **SD** |
| MTAD | 17.1364 | 1.16975 |
| Smear Clear | 19.1964 | 1.31468 |
| **p value** | **0.01\*** | |

**Table-2 Mean comparison of Ca/P ratio between irrigants within young group**

|  |  |  |
| --- | --- | --- |
| **Ca/P RATIO** | | |
| **Groups** | **Group 1**  **(Younger age group)** | |
| **Mean** | **SD** |
| MTAD | 1.5682 | 0.15452 |
| Smear Clear | 1.7164 | 0.14445 |
| **p value** | **0.02\*** | |

**Table-3 Mean comparison of phosphorous content between irrigants within old group**

|  |  |  |
| --- | --- | --- |
| **PHOSPHOROUS CONTENT** | | |
| **Groups** | **Group 2**  **(Older age group)** | |
| **Mean** | **SD** |
| MTAD | 12.7264 | 1.32706 |
| Smear Clear | 13.9127 | 1.90919 |
| **p value** | **0.03\*** | |

**DISCUSSION:**

Successful root canal treatment is focused on the complete removal of micro-organisms and their products by meticulous chemo-mechanical preparation followed by three-dimensional obturation of the root canal system[9].An inevitable outcome of any hand or rotary instrumentation is the creation of a substantial amount of debris shattered from mineralized tissues forming a non-homogenous structure, called the smear layer, on the walls of the cavity and the root canal. Clinically produced smear layers have an average depth of 1-5 microns (Goldman et.al.1981, Mader et.al. 1984).

Root canal therapy should not be simply the extirpation of the pulp and widening of the canal, but one should also focus on how to completely remove the loosely-attached smear layer, through irrigation of root canal space. However, irrigants used in the removal of smear layer produced during root canal preparation, might also affect the microhardness, chemical composition of root dentin[10].Any change in the mineral content such as Ca/P ratio may alter the standard proportion of the organic and inorganic components in the dentin which in turn affects the microhardness, permeability, solubility characteristics of dentin, sealing ability and adhesion of dental materials to the root canal dentin. Specifically, in case of root dentin, the irrigating agents react with the calcium ions in the hydroxyapatite crystals and can cause changes in the microstructure of the dentin by changing its Ca/P ratio[11].

The age-related changes of the dentin are also considered to be one of the crucial factors for the success of the endodontic treatment. The continuous deposition of peritubular dentin, consequent narrowing of dentinal tubules and decrease in the number of dentinal tubules are commonly seen among older individuals as these changes tend to correlate with the natural ageing process of humans[7].

Evidence shows that endodontic instruments are unable to contact all the parts of the root canal wall, leaving behind untouched areas. Thus, the use of chemical adjuncts is considered a ***“sine qua non”*** in root canal treatment.

Sodium hypochlorite the most commonly used irrigant, has the ability to dissolve the organic tissues. It has been reported that the use of NaOCl alone also altered the mineral content of root dentin causing mineral accumulation and increased amount of carbonate and reduced amount of phosphate[12].

The most common chelating solutions are based on Ethylene diaminetetraacetic acid (EDTA). EDTA reacts with the calcium ions present in root dentin and forms soluble calcium chelates and causes demineralization of dentin. The disadvantage is that it has negligible smear layer removal efficacy in the apical third which is a critical area for disinfection and obturation [13].

Later, MTAD (Mixture of Tetracycline Isomer, Acid and Detergent) a synergistic combination of 3% doxycycline, 4.25% citric acid, 0.5% polysorbate and detergent (Tween-80) introduced by Mahmoud Torabinejad had significantly improved smear layer removal as it is considered to be a chelating agent and also induces inconsiderable erosion[14]. In a recent investigation, De-Deus et al., reported significantly faster dissolution of inorganic material by both 5% citric acid and MTAD as compared with 17% EDTA[15].

A new formulation of EDTA, SmearClear containing 17% EDTA, cationic surfactant Cetrimide and a specific anionic surfactant Triton X-100 has gained increasing attention in recent years due to significant removal of smear layer in the apical third of root canal when compared to EDTA alone [16].

Surface alteration in root dentin may be due to the chemical changes brought by the irrigants resulting in alteration of Ca/P ratio [17]and these changes can be observed under Scanning Electron Microscope (SEM) whereas Energy Dispersive Spectroscopy (EDS) can be used for elemental analysis of tooth material to detect changes in Ca, P, Na, Mg and Ca/P ratio of root dentin[18].

In this study SEM/EDS is used which is based on the energy emitted in the form of X-ray photons, when the electrons from external source hit the atoms in a material, they generate characteristic X-rays of that element. This method allows fast and quantitative microanalysis, estimating the amount of mineral in a given tooth sample in a non-destructive manner[19].

In the present study, comparison of irrigants within younger age group revealed statistically significant difference in calcium content and Ca/P ratio with higher values for SmearClear sub group. This may be due to the presence of citric acid in MTAD which is a strong chelating agent and hence removed more calcium ions from root canal dentin[20].

Also, a statistically significant difference was observed in magnesium content between SmearClear and MTAD with higher values for MTAD sub group. This could be due to the binding of magnesium to phosphate, carbonate or the organic matrix[21]. This finding is in contrary with the study conducted by Eren SK et al., where the magnesium level changes were not significant when chelators are used as a final irrigant[19].

A statistically significant difference was observed in phosphorous content with higher values for SmearClear sub group. This is in accordance with Tay and Pasley who stated that mechanically instrumented intraradicular dentin after irrigation with EDTA or MTAD created a zone of demineralized collagen matrices in eroded dentin causing mineral loss with the mildly acidic MTAD being more aggressive than EDTA[22].

The organic matrix of dentin may act as a limiting factor in the dissolution of the inorganic component, thus reducing the decalcifying action of chelating agents over time. However, the low pH of irrigating solutions facilitates increased removal of major inorganic elements like calcium from the hydroxyapatite crystals[23]. Probably, this could be one of the reason for greater loss of minerals from MTAD (pH = 2.15) when compared to SmearClear (pH = 7.5-9).

Also, the current study is in line with the study conducted by Weerakoon AT et al, where the mineral contents were found to be higher among younger dentin samples. It could be ascribed to physiological ageing, where ageing increases dentin apatite density and distribution but not composition[24].

However, the present study acknowledges certain limitations. Firstly, the in vitro design of study is the major limitation along with the limited sample size. Blood, tissue remnants, temperature, various delivery and agitation devices may affect the action of chelating agents used during the root canal instrumentation.

Also, mineral content of dentin vary depending on the anatomical location, therefore separate measurements from each root third are to be considered and not of single point. Other factors like mineral content of the samples before treatment were not considered in the study due to logistic reasons. Future studies should include comparison of baseline with post-experimental mineral content of root dentin.

**CONCLUSION:**

Within the limitations of this in vitro investigation, the following conclusions were drawn:

* MTAD caused significantly greater loss of calcium, phosphorous, sodium and altered Ca/P ratio of root dentin among younger age group.
* On the other hand, loss of magnesium content was found to be higher within SmearClear sub group of younger age group (p=0.05).
* Similarly, among older age group, a significantly greater loss of all the minerals (calcium, phosphorous, magnesium and Ca/P ratio) were noted in MTAD sub group except for sodium content, wherein predominantly higher loss of sodium was observed in SmearClear sub group (p ≤ 0.05).

**ACKNOWLEDGEMENTS**

This research study did not receive any grants from funding agencies in the public, commercial and not for profit sectors.

**CONFLICT OF INTEREST**

No conflict of interest.

**REFERENCES:**

1. Ruddle CJ. Three-dimensional obturation of the root canal system. Dent Today. 1992;11(3):28, 30-3, 39.
2. Czonstkowsky M, Wilson EG, Holstein FA. The smear layer in endodontics. Dent Clin North Am. 1990;34(1):13-25.
3. White RR, Goldman M, Lin PS. The influence of the smeared layer upon dentinal tubule penetration by endodontic filling materials. Part II. J Endod. 1987;13:369-74.
4. Haapasalo M, Shen Y, Wang Z, Gao Y. Irrigation in endodontics. Br Dent J. 2014;216(6):299-303.
5. Siqueira JF Jr, Rôças I N, Favieri A, Lima K C. Chemomechanical reduction of the bacterial population in the root canal after instrumentation and irrigation with 1%, 2.5%, and 5.25% sodium hypochlorite. J Endod. 2000;26: 331-4.
6. Torabinejad M, Khademi AA, Babagoli J, Cho Y, Johnson WB, Bozhilov K, Kim J, Shabahang S. A new solution for the removal of the smear layer. J Endod. 2003;29(3):170-5.
7. Montoya C, Arango-Santander S, Peláez-Vargas A, Arola D, Ossa EA. Effect of aging on the microstructure, hardness and chemical composition of dentin. Arch Oral Biol. 2015;60(12):1811-20.
8. Eldarrat AH, High AS, Kale GM. Age-related changes in ac-impedance spectroscopy studies of normal human dentine: further investigations. J Mater Sci Mater Med. 2010;21:45–51.
9. Jagzap JB, Patil SS, Gade VJ, Chandhok DJ, Upagade MA, Thakur DA. Effectiveness of Three Different Irrigants - 17% Ethylenediaminetetraacetic Acid, Q-MIX, and Phytic Acid in Smear Layer Removal: A Comparative Scanning Electron Microscope Study. Contemp Clin Dent. 2017;8(3):459-63.
10. Dhawan R, Gupta A, Dhillon JS, Dhawan S, Sharma T, Batra D. Effect of different irrigating solutions with surfactants on the microhardness and smear layer removal of root canal dentin: An in vitro study. J Conserv Dent. 2019;22(5):454-8.
11. Zinge PR, Saraf PA, Ratnakar P, Karan S, Saraf SP, Hazari P. Assessment of effect of 1% phytic acid and 17% ethylenediaminetetraacetic acid on calcium ion loss of radicular dentin: An *ex vivo*study. J Conserv Dent. 2020;23(2):137-40.
12. Tsuda H, Ruben J, Arends J. Raman spectra of human dentin mineral. Eur J Oral Sci. 1996 Apr;104(2 ( Pt 1)):123-31.
13. Fraser JG. Chelating agents: their softening effect on root canal dentin. Oral Surg Oral Med Oral Pathol. 1974;37(5):803-11.
14. Zehnder M, Schmidlin P, Sener B, Waltimo T. Chelation in root canal therapy reconsidered. J Endod. 2005;31(11):817-20.
15. De-Deus G, Reis C, Fidel S, Fidel R, Paciornik S. Dentin demineralization when subjected to BioPure MTAD: a longitudinal and quantitative assessment. J Endod. 2007;33(11):1364-8.
16. Akcay I, Sen BH. The effect of surfactant addition to EDTA on microhardness of root dentin. J Endod. 2012;38(5):704-7.
17. Barón M, Llena C, Forner L, Palomares M, González-García C, Salmerón-Sánchez M. Nanostructural changes in dentine caused by endodontic irrigants. Med Oral Patol Oral Cir Bucal. 2013;18(4):e733-6.
18. Russ JC. Fundamentals of energy dispersive X-ray analysis: Butterworths monographs in materials. Butterworth-Heinemann; 2013.
19. Küçükkaya Eren S, Uzunoğlu E, Sezer B, Yılmaz Z, Boyacı İH. Mineral content analysis of root canal dentin using laser-induced breakdown spectroscopy. Restor Dent Endod. 2018;43(1):11-9.
20. Yadav HK, Tikku AP, Chandra A, Yadav RK, Patel DK. Efficacy of etidronic acid, BioPure MTAD and SmearClear in removing calcium ions from the root canal: An in vitro study. Eur J Dent. 2015;9(4):523-8.
21. Doğan H, Qalt S. Effects of chelating agents and sodium hypochlorite on mineral content of root dentin. J Endod. 2001;27(9):578-80.
22. Tay F.R., Pashley D.H. Ultrastructure of smear layer covered intraradicular dentin after irrigation with Biopure MTAD. J Endod*.*2006;32:18–21.
23. Poggio C, Dagna A, Vinci A, Beltrami R, Cucca L, Giardino L. Decalcifying capability of irrigating solutions on root canal dentin mineral content. Contemp Clin Dent. 2015;6(2):201-5.
24. Weerakoon AT, Cooper C, Meyers IA, Condon N, Sexton C, Thomson D, Ford PJ, Symons AL. Does dentine mineral change with anatomical location, microscopic site and patient age? J Struct Biol X. 2022;6:10006.